DAILY REPORT SUMMARY

TO:	Town of Addison						PROJECT:  Vitruvian Park - Addison, TX

16801 Westgrove Drive								Infrastructure Phase 1D

Addison, TX  75001-5190					PROJECT NO.: 99526 – 5

TECHNICIAN: Wade Geistweidt					REPORT DATE:

WEATHER: Clear & cool with light wind					REPOR	T NO.:

TIME ARRIVED:  8:30 AM						TEST DATE:  1-25-11

TIME DEPARTED:  6:00 PM

PROGRESS REPORT:

Wade Geistweidt with Kleinfelder continued observation of the Vitruvian Park Phase 1D project for the Town of Addison.  Austin Bridge and Roads crews are foreman by George, Arturo Gonzalez and Derek Dodson.  These crews consist of 15 people, 7 pieces of equipment, and numerous hand and power tools.  Austin’s first crew continued to work on PMD, over hangs, and continued installing the carrier pipes at the Ponte Bridge. Austin’s second crew place about 110 cubic yards of concrete for Abutment # 4 of the Bella Lane Bridge.  Kleinfelder obtained a sample from the first truck onsite to check the temperature and entrained air content.  Austin requested that TXI add hot water to the concrete mix to help maintain a minimum temperature of 50 degrees F.  The first load was tested for entrained air content and temperature.  The air content measured 6.4% and the temperature measured 74 degrees.  Derek Dodson called TXI’S dispatcher to have the hot water removed and the entrained air content adjusted down.  Kleinfelder cast two sets of 5 4X8 cylinders for this concrete placement today.  Major Jones from Halff and Associates was onsite to observe the concrete placement and perform a final reinforcing steel inspection.

COPIES TO:	Clay Barnett							KLEINFELDER

DRAFT