DAILY REPORT SUMMARY

TO:	Town of Addison						PROJECT:  Vitruvian Park - Addison, TX

16801 Westgrove Drive								Infrastructure Phase 1D

Addison, TX  75001-5190					PROJECT NO.: 99526 – 5

TECHNICIAN:	Wade Geistweidt					REPORT DATE:

WEATHER:  Cloudy with chance of rain and Strong South wind		REPOR	T NO.:

TIME ARRIVED:  8:15 AM						TEST DATE:  10-22-10

TIME DEPARTED: 5:45 PM

PROGRESS REPORT:

Wade Geistweidt with Kleinfelder continued observation of the Vitruvian Park Phase 1D project for the Town Of Addison.  Austin Bridge and Road crew is foreman by Derek Dodson and Arturo Gonzalez.  This crew consists of 15 people, 4 pieces of heavy equipment and numerous hand and power tools.  Austin Bridge and Road placed 75 cubic yards for Abutment # 1 North Wing wall on the Ponte Bridge.  Kleinfelder cast one set of 5 4X8 cylinders today.  Kleinfelder also monitor concrete temperatures for the mass placement.  This request was made by Halff and Associates. The temperature was measured upon delivery of concrete to the site.  The temperatures ranged for 75 degrees down to 65 degrees.  Halff had specified a mass concrete maximum placement temperature of 75 degrees.  Austin also placed temperature / maturity meters in the placement to record the internal temperature of the concrete.

COPIES TO:	Clay Barnett							KLEINFELDER

DRAFT