DAILY REPORT SUMMARY

TO:	Town of Addison						PROJECT:  Vitruvian Park - Addison, TX

16801 Westgrove Drive								Infrastructure Phase 1D

Addison, TX  75001-5190					PROJECT NO.: 99526 – 5

TECHNICIAN: Wade Geistweidt							REPORT DATE:

WEATHER: Clear with moderate North wind						REPOR	T NO.:

TIME ARRIVED: 8:15 AM 								TEST DATE:  12-8-10

TIME DEPARTED: 1:30 PM

PROGRESS REPORT:

Wade Geistweidt with Kleinfelder continued observation of the Vitruvian Park Phase 1D project for the Town of Addison.  Austin Bridge and Road crew is foreman by Derek Dodson and Arturo Gonzalez.  This crew consists of 15 people, 4 pieces of equipment, and numerous hand and power tools.  Austin’s crew continued to place the granular backfill between the wing and support walls on Abutment # 1 for the Ponte Bridge.  This crew was only able to place and test one lift of granular fill material today.  This crew also place 47 cubic yards for the stem wall on Abutment # 2 for the Ponte Bridge.  Austin also had a crew working on the Bella Lane Bridge.  This crew placed 9 cubic yards of concrete for the columns on bent # 3 of the Bella Lane Bridge.  They also worked on straitening the reinforcing steel for the columns on bent # 2 of the Bella Lane Bridge.  Kleinfelder performed 4 nuclear field density tests on the backfill and also cast one set of 5 4X8 cylinders for the concrete placement today.

COPIES TO:	Clay Barnett							KLEINFELDER

DRAFT