DAILY REPORT SUMMARY

TO:	Town of Addison						PROJECT:  Vitruvian Park - Addison, TX

16801 Westgrove Drive								Infrastructure Phase 1D

Addison, TX  75001-5190					PROJECT NO.: 99526 – 5

TECHNICIAN: Wade Geistweidt					REPORT DATE:

WEATHER: Clear							REPOR	T NO.:

TIME ARRIVED:  8:15 AM						TEST DATE:  4-29-11

TIME DEPARTED:  5:45 PM

PROGRESS REPORT:

Wade Geistweidt with Kleinfelder continued observation of the Vitruvian Park Phase 1D project for the Town of Addison.  Austin Bridge and Road crews are foreman by Arturo Gonzales, George, and Derek Dodson. These crews consist of 10 people, 7 pieces of equipment, and numerous hand and power tools.  Austin first and second crews worked together today on the Bella Lane and Ponte Ave Bridges.  This work included placing 20 cubic yards for the NE & SE sidewalk and brick paver bases at the Ponte Bridge.  This crew also continued forming the SW sidewalk and brick paver bases.  Kleinfelder had Ryan Jent from the Austin TX office onsite today to perform dry film thickness testing.  Mr. Jent performed testing on the left arch at the Ponte Bridge and both the left and right arches at the Bella Lane Bridge.  These were baseline readings on the zinc primer on the arches.  Mr. Jent captured some more pictures of rust bleeding through the zinc primer.  These areas have some concern do to low dry film thicknesses in these areas.  Mr. Jent will download these pictures and submit them to Mr. Robert Boswell for review.  Mr. Boswell will then make an interpretation and notify Mr. Geistweidt of how to proceed.  Mrs. Goethals from Carboline has only responded that she was forwarding the pictures from yesterday on to Carbolines Technical division.  Kleinfelder also cast one set of 5 4X8 cylinders today.

COPIES TO:	Clay Barnett							KLEINFELDER

DRAFT