DAILY REPORT SUMMARY

TO:	Town of Addison						PROJECT:  Vitruvian Park - Addison, TX

16801 Westgrove Drive								Infrastructure Phase 1D

Addison, TX  75001-5190					PROJECT NO.: 99526 – 5

TECHNICIAN: Wade Geistweidt					REPORT DATE:

WEATHER: Clear with light South wind					REPOR	T NO.:

TIME ARRIVED:  8:15 AM						TEST DATE:  5-26-11

TIME DEPARTED:  5:30 PM

PROGRESS REPORT:

Wade Geistweidt with Kleinfelder continued observation of the Vitruvian Park Phase 1D project for the Town of Addison.  Austin Bridge and Road crews are foreman by George, and Derek Dodson. These crews consist of 5 people, 5 pieces of equipment, and numerous hand and power tools.  Austin’s crew was tasked with sand blasting the weld seams for the bottom slide plates on the Bella Lane Bridge.  Austin also installed the Carboguard 501 filler product over the remaining three weld seams on the Bella Lane Bridge.  Austin planned to have Don Gandy with Scott Derr Painting onsite to reapply the zinc primer coating on the mock up section of the arch this afternoon.  Mr. Gandy had not arrived onsite by 5 PM today.  Austin rewrapped the bare steel on the arches so they would not flash rust over night.  UDR, the Town of Addison, Nathan D Maier, Austin Bridge and Road, and a Sika representative all met on the Bella Lane Bridge to discuss some cracking issues that have arisen.  Sika is developing a solution to apply to the bridge deck to seal the cracks.

COPIES TO:	Clay Barnett							KLEINFELDER

DRAFT