DAILY REPORT SUMMARY

TO:	Town of Addison						PROJECT:  Vitruvian Park - Addison, TX

16801 Westgrove Drive								Infrastructure Phase 1D

Addison, TX  75001-5190					PROJECT NO.: 99526 – 5

TECHNICIAN: Wade Geistweidt					REPORT DATE:

WEATHER: Cloudy with strong South wind				REPOR	T NO.:

TIME ARRIVED:  8:15 AM						TEST DATE:  5-31-11

TIME DEPARTED:  5:00 PM

PROGRESS REPORT:

Wade Geistweidt with Kleinfelder continued observation of the Vitruvian Park Phase 1D project for the Town of Addison.  Austin Bridge and Road crews are foreman by George, and Derek Dodson. These crews consist of 5 people, 3 pieces of equipment, and numerous hand and power tools.  Austin’s crew was tasked with reapplying the Carboguard 501 filler product on the weld seams for both the Ponte and Bella Lane Bridges.  This was done to level out the remaining low areas around the weld seams.  Austin did have a painting crew with Scott Derr Painting onsite to apply the top coat on the mock up at the Bella Lane Bridge today.  This top coat was supposed to be applied on Saturday; however the painter applied the intermediate coat to the mock up on Saturday again.  Nancy Cline with the Town of Addison was invited to the site by Eric Little of UDR to approve the minimum standard that would be accepted for these arches.

COPIES TO:	Clay Barnett							KLEINFELDER

DRAFT