DAILY REPORT SUMMARY

TO:	Town of Addison						PROJECT:  Vitruvian Park - Addison, TX

16801 Westgrove Drive								Infrastructure Phase 1D

Addison, TX  75001-5190					PROJECT NO.: 99526 – 5

TECHNICIAN: Wade Geistweidt					REPORT DATE:

WEATHER: Cloudy with strong South wind and HOT			REPOR	T NO.:

TIME ARRIVED:  8:15 AM						TEST DATE:  6-10-11

TIME DEPARTED:  5:00 PM

PROGRESS REPORT:

Wade Geistweidt with Kleinfelder continued observation of the Vitruvian Park Phase 1D project for the Town of Addison.  Austin Bridge and Road crews are foreman by George, and Andrew Harper. These crews consist of 4 people, 2 pieces of equipment, and numerous hand and power tools.  Austin crew had completed the chipping required on abutment # 2 of the Ponte Bridge.  Austin placed 3 cubic yards of concrete for the drainage repair which was bonded to the existing concrete with a two part epoxy bonding agent.  Kleinfelder observed Austin place and finish these repair areas and gave suggestions on how to check drainage off the bridge and approach slab. The painting crew from Scott Derr Painting arrived onsite to continue sanding the right arch of the Ponte Bridge at 10:21 AM.  This crew worked through out the day to sand the ruff paint to a smooth surface. There was no painting performed today on either of the bridges.  Kleinfelder cast one set of 5 4X8 cylinders for the concrete placement today.

COPIES TO:	Clay Barnett							KLEINFELDER

DRAFT