DAILY REPORT SUMMARY

TO:	Town of Addison						PROJECT:  Vitruvian Park - Addison, TX

16801 Westgrove Drive								Infrastructure Phase 1D

Addison, TX  75001-5190					PROJECT NO.: 99526 – 5

TECHNICIAN: Wade Geistweidt					REPORT DATE:

WEATHER: Cloudy with strong South wind and HOT			REPOR	T NO.:

TIME ARRIVED:  8:15 AM						TEST DATE:  6-6-11

TIME DEPARTED:  5:00 PM

PROGRESS REPORT:

Wade Geistweidt and David Hernandez with Kleinfelder continued observation of the Vitruvian Park Phase 1D project for the Town of Addison.  Austin Bridge and Road crews are foreman by George, and Derek Dodson. These crews consist of 4 people, 3 pieces of equipment, and numerous hand and power tools.  Austin’s crew was tasked with sanding the Carboguard 501 filler product on the weld seams for both the Ponte Ave Bridge arches.  This was done to level out the remaining low areas around the weld seams.  The painting crew from Scott Derr Painting arrived onsite to begin painting the Bella Lane arches at 9:20 AM.  Wade Geistweidt with Kleinfelder spoke with this crew to obtain their plan for the day.  The painters said they planned to remove all the rust from any of the damaged or repaired areas and then apply the zinc primer coat.  After this primer coat had dried sufficiently they planned to power wash the remainder of the arch until Kleinfelder representative approved the degree of cleaning.  Kleinfelder approved the level of cleaning at 4:45 PM today.  Scott Derr crew plans to be back onsite tomorrow and continue cleaning on the right arch of the Bella Lane Bridge.  After the right arch is clean the painters plan to begin applying the intermediate coat to the left arch as the right arch dries.

COPIES TO:	Clay Barnett							KLEINFELDER

DRAFT