DAILY REPORT SUMMARY

TO:	Town of Addison						PROJECT:  Vitruvian Park - Addison, TX

16801 Westgrove Drive								Infrastructure Phase 1D

Addison, TX  75001-5190					PROJECT NO.: 99526 – 5

TECHNICIAN: Wade Geistweidt					REPORT DATE:

WEATHER: Cloudy with strong South wind and HOT			REPOR	T NO.:

TIME ARRIVED:  8:15 AM						TEST DATE:  6-8-11

TIME DEPARTED:  5:20 PM

PROGRESS REPORT:

Wade Geistweidt and David Hernandez with Kleinfelder continued observation of the Vitruvian Park Phase 1D project for the Town of Addison.  Austin Bridge and Road crews are foreman by George, and Derek Dodson. These crews consist of 4 people, 3 pieces of equipment, and numerous hand and power tools.  Austin’s crew was tasked with sanding the Carboguard 501 filler product on the weld seams for both the Ponte Ave Bridge arches.  This was done to level out the remaining low areas around the weld seams.  The painting crew from Scott Derr Painting arrived onsite to begin painting the Bella Lane arches at 9:30 AM.  David Hernandez had spoke with this crew yesterday about being onsite at 7AM to begin painting while the steel and ambient temperatures were still relatively cool. The painters began mixing paint by 10:00 AM and were ready to begin painting by 10:15 AM.  The painters applied an intermediate coat of paint to the right arch on the Bella Lane Bridge.  After this was completed the painters left for lunch.  Upon arrival back from lunch the painters determined it was too windy to apply the topping coat to the arches on the Bella Lane Bridge.  After this determination was made the painters left the site at 1:30 PM.  David Hernandez left the site at about 2:00 PM.

COPIES TO:	Clay Barnett							KLEINFELDER

DRAFT