DAILY REPORT SUMMARY

TO:	Town of Addison						PROJECT:  Vitruvian Park - Addison, TX

16801 Westgrove Drive								Infrastructure Phase 1D

Addison, TX  75001-5190					PROJECT NO.: 99526 – 5

TECHNICIAN: Wade Geistweidt					REPORT DATE:

WEATHER: Clear with moderate South wind and HOT			REPOR	T NO.:

TIME ARRIVED:  8:00 AM						TEST DATE:  7-12-11

TIME DEPARTED:  11:30 PM

PROGRESS REPORT:

Wade Geistweidt with Kleinfelder continued observation of the Vitruvian Park Phase 1D project for the Town of Addison.  Austin Bridge and Road had there painting contractor Scott Derr Painting onsite today.  The painting crew from Scott Derr Painting arrived onsite about 8:30 AM.  This crew applied one coat of Carboline Carbothane 130 Clear Coat today on the left arch of the Ponte Ave Bridge.  This clear coat had a purple fugitive dye mixed with it so Luis with Scott Derr Painting could see where he had already painted.  Kleinfelder began monitoring temperatures at 9:00 AM the steel temperature was 90 degrees, and by 10:00 AM it had reached 106 degrees.  Scott Derrs crew had completed application of the clear coat by 11:30 AM today.  Kleinfelder referred to the National Weather Service at the Addison Airport for current temperature readings through out the day.

COPIES TO:	Clay Barnett							KLEINFELDER

DRAFT